规 格 承 认 书 SPECIFICATION FOR APPROVAL 产 品 名 称: CBB11金属箔式聚丙烯膜介质电容器 Product Name: CBB11 foil type polypropylene film capacitor 产 品 型 号: CBB11 Product Type: CBB11 产 品 编 码: Product Code: 客 户 名 称: Customers Name: 客 户 编 码: Customers Code: 日 期: 2018.12.13 Issue Date: 2018.12.13 浙江七星电子股份有限公司 Zhejiang Qixing Electronics Corp ., Ltd. 地址：浙江省长兴县新槐镇开发区发展大道50号 ADD:Changxingxian Huaikan Dev Zone, 50 Development Rd, Changxing, Zhejiang Tel：0572-6295698 Fax：0572-6295700

CBB11 聚酯膜电容器

CBB11 foil type polypropylene film capacitor

■ 特点                                           ■ Characteristic:

●高频损耗小、绝缘电阻高                          ●Low loss at high frequency and high insulation resistance

●体积小、重量轻                                  ●Small in size and light in weight

● 内部升温小，稳定性好

■主要用途                                        ■ Main purpose

● 旁路，隔直，耦合，退耦                         ● Bypass, partition, coupling, decoupling.

● 脉冲，逻辑，定时，紧凑型节能灯                 ● Pulse, logic, timing, compact CFL.

●LCD监视器整流，汽车直流马达抑制干扰            ●LCD monitor rectification, automotive DC

motor suppression interference

- 技术要求 Technical requirements

| 引用标准 Reference criteria | GB6349 / SJ/T 10786 |
| --- | --- |
| 气候类别 Climate category | 40/105/21 |
| 额定温度 Rated temperature | 85℃ |
| 工作温度 Operating temperature | -55℃~105℃ 〔+85℃to+105℃：decreasing factor 1.25% per℃ for Ur(dc) 〕 |
| 额定电压 Rated voltage 〔DC〕 | 100V, 400V, 630V, 1000V,1200V, 1500V |
| 电容量范围 Electricity capacity range | 220PF~0.068μF |
| 电容量偏差 Capacitance deviation | ±5%〔J〕,±10%〔K〕,±20%〔M〕 |
| 耐电压 Voltage resistance | 2.5Ur 〔2s〕无飞弧或击穿 |
| 损耗角正切值 Loss angle tangent | 频率Frequency | Cn≤0.1μF | C＞0.1μF |
|  | 1KHz | tgδ≤0.0010 | tgδ≤0.0015 |
|  | 10KHz | tgδ≤0.0020 | tgδ≤0.0025 |
| 绝缘电阻 Insulation resistance | Ur < 500V | R≥30000MΩ Cn≤0.1μF | +25±5℃ 100V 1min |
|  |  | IR≥10000S Cn＞0.1μF |  |
|  | Ur≥ 500V | R≥35000 MΩ Cn≤0.1μF | +25±5℃ 500V 1min |
|  |  | IR≥15000S Cn＞0.1μF |  |

■电容器外形尺寸Capacitor dimensions

| 100VDC | 400VDC |
| --- | --- |
| 电容量 CAP | 电容器外形尺寸Capacitor dimensions | 电容器代码 Part number | 电容量 CAP | 电容器外形尺寸Capacitor dimensions | 电容器代码 Part number |
|  | T | H | W | P | Φd |  |  | T | H | W | P | Φd |  |
| 1000PF | 4 | 11 | 6.5 | 3.8 | 0.5 | B110100V102J03NLAQ | 1000PF | 4.5 | 12.5 | 6.5 | 5 | 0.5 | B110400V102J05ANLAQ |
| 1500 | 4.5 | 13 | 7.5 | 3.8 | 0.5 | B110100V152J03NLAQ | 1500 | 5.5 | 12.5 | 6.5 | 5 | 0.5 | B110400V152J05ANLAQ |
| 2200 | 4.5 | 13 | 7.5 | 4.0 | 0.5 | B110100V222J04 NLAQ | 2200 | 5.5 | 12.5 | 7.5 | 5 | 0.5 | B110400V222J05ANLAQ |
| 2700 | 4.5 | 13 | 7.5 | 4.0 | 0.5 | B110100V272 J04 NLAQ | 2700 | 5.5 | 13.0 | 7.5 | 5 | 0.5 | B110400V272J05ANLAQ |
| 3300 | 4.5 | 13 | 8 | 4.5 | 0.5 | B110100V332J4A NLAQ | 3300 | 5.5 | 13.0 | 8.0 | 5 | 0.5 | B110400V332J05ANLAQ |
| 4700 | 5.0 | 13 | 8 | 4.5 | 0.5 | B110100V472J4A NLAQ | 4700 | 6.0 | 13.0 | 8.0 | 6.5 | 0.5 | B110400V472J6AANLAQ |
| 6800 | 5.0 | 13 | 8 | 4.5 | 0.5 | B110100V682J4ANLAQ | 6800 | 7.0 | 14.0 | 9.0 | 7.5 | 0.5 | B110400V680J7AANLAQ |
| 0.01μF | 5.5 | 12 | 8.5 | 5.0 | 0.5 | B110100V103J05NLAQ | 0.01μF | 8.0 | 14.0 | 11 | 7.5 | 0.5 | B110400V103J7AANLAQ |
| 0.012 | 5.5 | 12 | 8.5 | 5.0 | 0.5 | B110100V123 J05NLAQ | 0.012 | 8.0 | 14.0 | 11 | 7.5 | 0.5 | B110400V123J7AANLAQ |
| 0.015 | 5.5 | 12 | 8.5 | 5.5 | 0.5 | B110100V153 J5ANLAQ | 0.015 | 8.0 | 15.0 | 11 | 7.5 | 0.5 | B110400V153J7AANLAQ |
| 0.022 | 5.5 | 12 | 8.5 | 6.0 | 0.5 | B110100V223 J06NLAQ | 0.022 | 8.0 | 15.0 | 12 | 7.5 | 0.6 | B110400V223J7AANLAQ |
| 0.033 | 6.0 | 13 | 10 | 6.0 | 0.5 | B110100V333 J06NLAQ | 0.033 | 8.5 | 15.0 | 13 | 7.5 | 0.6 | B110400V333J7AANLAQ |
| 0.047 | 6.5 | 13 | 10 | 6.5 | 0.5 | B110100V473 J6ANLAQ |  |  |  |  |  |  |  |
| 0.068 | 7.5 | 13 | 11 | 6.5 | 0.5 | B110100V683 J6ANLAQ |  |  |  |  |  |  |  |
| 630VDC | 1000VDC |
| 电容量 CAP | 电容器外形尺寸 Capacitor dimensions | 电容器代码 Part number | 电容量 CAP | 电容器外形尺寸 Capacitor dimensions | 电容器代码 Part number |
|  | T | H | W | P | Φd |  |  | T | H | W | P | Φd |  |
| 220PF | 4.0 | 12 | 6.0 | 4.0 | 0.5 | B110630V221K04NLAQ | 220PF | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111000V221 K04NLAQ |
| 330 | 4.0 | 12 | 6.0 | 5.0 | 0.5 | B110630V 331K05NLAQ | 330 | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111000V331 K04NLAQ |
| 470 | 4.0 | 12 | 6.0 | 5.0 | 0.5 | B110630V471 K05NLAQ | 470 | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111000V471 K04NLAQ |
| 680 | 4.0 | 12 | 6.0 | 5.0 | 0.5 | B110630V681 K05NLAQ | 680 | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111000V 681K04NLAQ |
| 1000 | 4.5 | 12.5 | 6.5 | 5.0 | 0.5 | B110630V102 K05NLAQ | 1000 | 5.5 | 13.0 | 7.0 | 4.5 | 0.5 | B111000V 102K4ANLAQ |
| 1500 | 5.5 | 12.5 | 7.5 | 5.0 | 0.5 | B110630V152 K05NLAQ | 1500 | 6.0 | 14.0 | 8.5 | 5.0 | 0.5 | B111000V 152K05NLAQ |
| 2200 | 5.5 | 12.5 | 8.0 | 5.0 | 0.5 | B110630V222 K05NLAQ | 2200 | 6.0 | 14.0 | 9.0 | 5.0 | 0.5 | B111000V 222K05NLAQ |
| 3300 | 5.5 | 13 | 9.0 | 5.0 | 0.5 | B110630V332 K05NLAQ | 3300 | 6.5 | 15.0 | 9.0 | 6.0 | 0.5 | B111000V 332K06NLAQ |
| 4700 | 6.0 | 13 | 9.5 | 7.5 | 0.5 | B110630V472 K7ANLAQ | 4700 | 7.5 | 15.5 | 10 | 6.0 | 0.5 | B111000V 472K06NLAQ |
| 6800 | 7.0 | 14 | 9.5 | 7.5 | 0.5 | B110630V682 K7ANLAQ | 6800 | 8.0 | 16.0 | 12 | 8.0 | 0.5 | B111000V 682K08NLAQ |
| 8200 | 7.0 | 15 | 11 | 7.5 | 0.5 | B110630V 822K7ANLAQ | 8200 | 8.5 | 16.0 | 13 | 8.0 | 0.5 | B111000V 822K08NLAQ |
| 0.01μF | 8.0 | 15 | 11 | 7.5 | 0.5 | B110630V 103K7ANLAQ | 0.01μF | 9.0 | 16.0 | 13 | 8.0 | 0.5 | B111000V 103K08NLAQ |
| 0.015 | 8.0 | 16 | 12 | 7.5 | 0.6 | B110630V 153K7ANLAQ | 0.015 | 9.0 | 16.0 | 14 | 9.0 | 0.6 | B111000V 153K09NLAQ |
| 0.022 | 8.0 | 17.5 | 12 | 7.5 | 0.6 | B110630V223 K7ANLAQ | 0.022 | 9.0 | 16.0 | 14 | 9.0 | 0.6 | B111000V 223K09NLAQ |

| 1200VDC | 1500VDC |
| --- | --- |
| 电容量 CAP | 电容器外形尺寸Capacitor dimensions | 电容器代码 Part number | 电容量 CAP | 电容器外形尺寸Capacitor dimensions | 电容器代码 Part number |
|  | T | H | W | P | Φd |  |  | T | H | W | P | Φd |  |
| 220PF | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111200V221K04NLAQ | 220PF | 5.0 | 12.5 | 6.5 | 4.5 | 0.5 | B111500V221K4ANLAQ |
| 330 | 5.0 | 12.5 | 6.5 | 4.0 | 0.5 | B111200V331K04NLAQ | 330 | 5.0 | 12.5 | 6.5 | 4.5 | 0.5 | B111500V331K4ANLAQ |
| 470 | 5.0 | 12.5 | 6.5 | 4.5 | 0.5 | B111200V471K4ANLAQ | 470 | 5.0 | 12.5 | 6.5 | 4.5 | 0.5 | B111500V471K4ANLAQ |
| 680 | 5.0 | 12.5 | 7.0 | 4.5 | 0.5 | B111200V681K4ANLAQ | 680 | 5.0 | 12.5 | 7.0 | 5.0 | 0.5 | B111500V681K05NLAQ |
| 820 | 5.5 | 13.0 | 7.0 | 4.5 | 0.5 | B111200V821K4ANLAQ | 820 | 5.5 | 13.0 | 7.0 | 5.0 | 0.5 | B111500V821K05NLAQ |
| 1000 | 5.5 | 13.0 | 8.0 | 5.0 | 0.5 | B111200V102K05NLAQ | 1000 | 5.5 | 13.0 | 8.0 | 5.0 | 0.5 | B111500V102K05NLAQ |
| 1500 | 6.0 | 13.0 | 8.0 | 5.0 | 0.5 | B111200V152K05NLAQ | 1500 | 6.0 | 13.0 | 8.0 | 5.0 | 0.5 | B111500V152K05NLAQ |
| 2200 | 6.0 | 13.0 | 8.5 | 5.0 | 0.5 | B111200V222K05NLAQ | 2200 | 6.0 | 13.0 | 8.5 | 5.0 | 0.5 | B111500V222K05NLAQ |
| 3300 | 6.5 | 13.0 | 9.0 | 5.0 | 0.5 | B111200V332K05NLAQ | 3300 | 6.5 | 13.0 | 9.0 | 5.0 | 0.5 | B111500V332K05NLAQ |
| 4700 | 7.5 | 15.5 | 10 | 7.5 | 0.5 | B111200V472K7ANLAQ |  |  |  |  |  |  |  |
| 6800 | 8.0 | 15.5 | 12 | 7.5 | 0.5 | B111200V682K7ANLAQ |  |  |  |  |  |  |  |
| 8200 | 8.5 | 15.5 | 13 | 8.0 | 0.5 | B111200V822K08NLAQ |  |  |  |  |  |  |  |
| 0.01μF | 9.0 | 16.5 | 13 | 8.5 | 0.6 | B111200V103K8ANLAQ |  |  |  |  |  |  |  |
| 0.015 | 9.0 | 16.5 | 14 | 9.0 | 0.6 | B111200V153K09NLAQ |  |  |  |  |  |  |  |
| 0.022 | 9.0 | 16.5 | 14 | 9.0 | 0.6 | B111200V223K09NLAQ |  |  |  |  |  |  |  |

dering